RFQ-TKM-005-2020

Procurement, supply and installation of an extrusion line for the production of high-density polyethylene membrane (HDPE) for the UNDP / GEF project “Energy Efficiency and Renewable Energy for Sustainable Water Management in Turkmenistan”.

| № | Date | Question | Answer |
| --- | --- | --- | --- |
| Round 1 | March 16, 2020 | Questions related to technical parameters: Productivity: 100 - 200 kg/h - This is very small for a 2000 x 0.5 mm geomembrane. 120/36 185kW normally performs a real productivity of 400-450 kg/h. Will it be considered as a non-compliance with the RFQ terms if the productivity of the line is higher than specified in the technical specifications? | Higher productivity will not be considered as a non-compliance. |
|  |  | Questions related to equipment: Position No. 1: Melting pump? It is not in the list of equipment, is it required or not? | Melting pump is not necessary. However, it is desirable. Other things being equal, offers with a pump will be better, but to make a membrane with the width of 2 m no pump is required. |
|  |  | Cooling chiller – Here we are talking about a thermostat for thermal control of three-roll calender with a water-cooling agent, and not an external chiller for supplying cold water, right? | Yes, to control the temperature of the three-roll calender. |
|  |  | Device for trimming and crushing the edges - Do you need an online crusher to crush edges or not? | It is possible to have online edge winding device and crush it later using offline crusher. |
|  |  | Polymer Crusher - Is it a separate crusher that works separately from the line? Or is it an online crusher? | An offline crusher will be used. |
|  |  | A device for manufacturing of pellets from recycled materials - Is this a separate granulation line? | Yes, it is the smallest and most simple granulator. |
|  |  | Position No. 6: Hot wedge geomembrane welding machine - it is called a thermal iron, is it necessary to offer or not? | Mandatory required! It is impossible to perform a proper stacking without it. |