|  | General Description |
| --- | --- |
| Qty( net unit) | Nylon fishing nets (gillnets) fully assembled with head and foot rope, buoys and sinkers | Nylon fishing nets |
|  | Description |  |
|  |  | Netting |
|  | Nylon multi-filament twine | Material |
|  | Grey or Greyish green | Color |
|  | 1463 meshes (164.6 meters) (90fathoms) | Length |
|  | 100 meshes (11.25 meters) (6.15 fathoms) when hung | Depth |
|  | 112.5 mm (4.5 “) | Mesh size (stretched mesh) |
|  | 210D/30 | Twine size |
|  | Double | Type of knot |
|  | 0.56 | Hanging ratio |
|  | Depth-wise | Director of knot |
|  | Double | Selvedge top, sides and bottom |
|  | Weight of the net should not be lesser than 30 kg before the net hung to ropes and fitted with floats and weights | Weight of twine/net unit |
|  | Ropes |
| 1 | Polyethylene twisted 9 mm diameter, 200-yard length, and black color. | Float Line (Head Rope) |
| 1 | Polyethylene twisted 7 mm diameter, 200-yard length, and black color. | Sinker Line (Foot Rope) |
| 2 pieces | Each vertical end of both sides of fishing net shall be fitted with 25-yard-long rope made of a 12 mm diameter multi-ply polyethylene rope, any color. | Side Ropes (buoy lines) |
|  | Floats |
| 100 pieces | PVC floats, oval in shape, with size of (50mm ± (10%) x 80mm ± (10%)), weight of 45g±(10%), buoyancy of 100g± (10%), with a central hole to exactly fit 9 mm diameter rope, and it should suit for salt water at depth of 100m-150m. Evenly spaced on head rope (approximately 1.0metres apart) |  |
| 2 pieces | Ethylene vinyl acetate (EVA) buoy of cylindrical type with size of 201 mm45g± (10%)long and 176 mm45g± (10%) diameter, weight of 510g± (10%), with a buoyancy of 3.5 kg± (10%) and with a central hole to exactly fit 12mm rope. |  |
| 25 | Lead sinkers/weights, cube shaped or any other shape, evenly spaced on footrope (approximately 2.0 meters apart) and each weighing 250 g, and with a central hole to exactly fit 7 mm diameter rope. | Sinkers |
|  | The footrope and weights and the vertical end ropes will be attached to the net using 210D/30-nylon thread. | Assembling |
| 1 spool | Each net should come with a 1-lb (spool of 201D/30 nylon twine for additional fastening and mending, grey color. | Additional twine |